Architectural Components Group, Inc.

521 George St.

Marshfield, MO 65706

417-869-6777  /  417-869-7888 fax

info@acgiwood.com / acgiwood.com

ARCHITECTURAL SPECIFICATIONS FOR

WOOD COFFER CEILING SYSTEM

[Project Name]

[Project Location]

PART 1 — GENERAL

1.1 Description of Work:

- Work Included: Provide Architectural Components Group, Inc. Wood Coffer ceiling system, product CF1-2424 or CF2-2424 where shown on architectural drawings, and as specified in this specification.

1.2 Quality Assurance:

- Architectural Components Group, Inc. CF1-2424 or CF2-2424 Wood Coffer ceiling system for this project shall maintain the quality as instituted by the architect or A.W.I.

- Design Criteria: Manufacture of CF1-2424 or CF2-2424 Wood Coffer shall be installed true and plumb to within manufacturing tolerance of 1/8” within 8’ of length.

- Product Construction: Wood shall be kiln dried to 10%. Cracking, checking and warpage of members will not be acceptable.

1.3 Submittals:

- Technical Data: Submit manufacturer’s data and installation instructions.

- Shop Drawings: Submit 4 copies of shop drawings showing all areas involved, attachment conditions and perimeter circumstances.

- Submittal Sample: Submit 1 product sample for approval by architect.

1.4 Delivery, Storage and Handling

- Material must be stored and installed only in secured ambient environment (humidity min. 25% - max. 55%, temperature not to exceed 86 degrees).

- Windows, doors and all wet-work must be completed before unpacking and installation. Handle carefully to avoid damage.

PART 2 — PRODUCTS

2.1 Acceptable Manufacturer

Architectural Components Group, Inc., 521 George Street, Marshfield, MO 65706

Phone (417) 869-6777	Fax (417) 869-7888

2.2 Product Type

- Product Configuration: Wood Coffer ceiling system, product series 1 CF1-2424 or series 2 CF2-2424. Wood Coffers shall be provided in a panel size of 24” wide x 24” length.

- Species:

  - Face veneer shall consist of [desired wood veneer species, e.g., maple plain-sliced, book-matched; or paint].

  - Molding shall consist of [desired solid wood species, e.g., maple; or paint].

- Finish: Wood veneer finish shall utilize ACGI clear finish with satin sheen or specify stain to match architect sample.

- Certification: Wood veneer, core and solid wood shall or shall not be FSC certified. If FSC, Chain of Custody shall or shall not be provided.

- Substrate material shall or shall not be manufactured with no added urea formaldehyde.

- Attachment System: Coffer Ceiling System shall be suspended according to manufacturers’ suggested method of suspension as per the design details provided in the plans.

- Fire Rating: Allegro panels shall be constructed with components achieving a Class A (flame spread <25, smoke developed <450) rating.

PART 3 — EXECUTION

3.1 Installation

- Wood Coffer Ceiling System shall be handled and installed with care in order to prevent surface and structure damage. Field cutting shall be kept to a minimum and performed as recommended by manufacturer.

- The ceiling system shall be suspended by HD T-grid with main runners on 2’ centers and cross T’s every 2’.

- Panels shall be installed by sliding each panel into the T-grid flanges.

PART 4 — WARRANTY

4.1 Product Warranty

- Architectural Components Group, Inc. shall warranty the Wood Coffer Ceiling System against manufacturer’s defects up to one year. Changes in finish or dimensions due to ultra violet light, excessive temperature or humidity conditions and/or abuse of any kind shall void any warranties from ACGI.

- Install conditions for the area should remain for the proper occupied conditions of humidity and temperature (humidity min. 25% - max. 55%, temperature not to exceed 86 degrees).